## Slide 1: Superconductors, light, and the “age of of cognition”
Jeff Chiles, Sonia Buckley, Adam McCaughan, Saeed Khan, Bryce Primavera,
Rich Mirin, Sae Woo Nam, Jeff Shainline
NIST, Physical Measurement Laboratory
“Super” Neuromorphic Computing with Photonic and Superconducting Devices

## Slide 2: High Performance Single Photon Detectors
Superconducting nanowire single photon detector
Superconducting Transistion-Edge Sensors
Microwave Kinetic Inductance Detectors
Conventional Applications
  Advanced sensors for astronomy and astrophysics
  High Energy Physics – rare particle event searches
  Quantum Information / Quantum Computation

## Slide 3: Photonic Quantum Information Requirements
 | Quantum Communication | Quantum Computing (Photonic) | Quantum Computing (atoms) | Entanglement-based random numbers
Wavelength | 1550 nm | Visible, Near-IR | UV | Near-IR
Detection Efficiency | As high as possible | As high as possible | >80% | >67%
Dark / Background counts | As low as possible
Timing jitter | As low as possible
Maximum count rate | As high as possible

## Slide 4: Conventional Single-Photon Detectors
Commercially available
Relatively inexpensive
M. D. Eisaman, J. Fan, A. Migdall, and S. V. Polyakov, Rev. Sci. Instrum. 82, 071101 (2011)

## Slide 5: Low Temperature Physics = High Performance
No afterpulsing problems
Excellent prospects for longer wavelengths
TES: Transition Edge Sensor
SNSPD: Superconducting Nanowire Single Photon Detector

## Slide 6: Superconducting Nanowire Single Photon Detectors:
ultra-thin (2nm to 8nm)
Anomolous kinetic inductance
NbN, NbTiN
  2K operating temperature
  ~80nm wide
New materials:
W-Si, Mo-Si, Mo-Ge
  1K operating temperature
  ~150nm
5 microns wide

## Slide 7: Simplicity of Superconducting Nanowire Single Photoncs Detectors
X
Simple Readout
Bias versus Efficiency / counts

## Slide 8
Air
aSi
SiO2
aSi
SiO2
Au
Substrate
Incoming photons
Single Pixel Devices
2.5 mm
Available Commercially now !!!
60 nm
100 nm
Notes: 8

## Slide 9: Future of Computing
High Performance Computing. (HPC)
  Traditional model of computation
Quantum Computing and Networking (QC)
  Can outperform HPC in some tasks
Neuromorphic Computing (NC)
  “Neuroscience” inspired architecture
  Dedicated Hardware

## Slide 10: Structure of a Biological Neuron
https://www.khanacademy.org/science/biology/human-biology/neuron-nervous-system/a/the-synapse
http://spie.org/news/5681-dendritic-plateau-potentials-modulate-neuronal-function?SSO=1
From:Wikipedia
DENDRITES

## Slide 11: Fast Introduction to Neural Networks
Artificial Neuron
Network of Neurons
http://www.asimovinstitute.org/neural-network-zoo/
Input Cell / Layer
Hidden Cell / Layer
Output Cell / Layer
S
F(x)
w1
w2
w3
x1
x2
x3
b
Summing
Node
Synaptic
Weights
inputs
Activation
Function

## Slide 12: Supervised Learning
Untrained
Neural Network
cat
not
cat
✅
Trained
Neural Network
Inference
New
Data
Training
✓
✓

## Slide 13: Machine learning hardware
Today, there is large demand to perform “neural network” operations
  Image Classification
  Speech Recognition
  Natural Language Processing: “translation”
Dedicated Neuromorphic Hardware
Other Technology platforms Neuromorphic have attracted venture interest
Bill Gates
TrueNorth, IBM
see Merolla et al.,
Science, 2011.
Notes: Plug Nick’s talk
I don’t have to make a case that Moore’s law is ending. There is a belief that electronics will not be able to supply what is needed – nothing is on the way. This was not true in 1980s. GPUs and FPGAs

## Slide 14
2nd and 3rd Generation Neural Networks
2nd Generation: “Proven”
Limited Biological “inspiration”
Matrix-vector multiplication
Seeking weight matrix
Trained by supervisory system
Limited History
Task specific
3rd Generation: “Less Proven”
More Biologically inspired
Information in dynamical state
Spiking neurons communicate in rate and timing
Potential for learning without supervision
Information integrated across space and time
General cognitive systems

## Slide 15: Question: Why do we need Generation 3? Answer: Energy Efficiency and Size
https://arxiv.org/abs/1906.02243v1
“How do you make the largest scale artificial neural network?”
  Human Brain:
    10 billion neurons
    1 neuron fans out to 10,000 neurons
What are the fundamental limits?
How do you evaluate the performance?
How do physical characteristics of the devices relate to the performance of the neuromorphic computer?

## Slide 16: Spiking Neural Networks / Dedicated Hardware
Biologically Inspired
  Spiking Signals, Energy Efficient
  Rate and Time encoding
Differentiated local processing
Information integration across:
  Space (network structure)
  Time (dynamics)
  Experience (plasticity)
Can we get to a size scale for “Cognitive” Systems?

## Slide 17: Energy and Training Targets
Power
2500 kCal/day = 100Watts
Clock speed
1 Hz to 1kHz
Training time
18 years
Power
100 kW to 1 MW
Clock speed
1 Mhz to 10MHz
Training time
1 week
Human
Artificial
Notes: Dominated by light source
1fJ is needed per synapse
10^10 neurons * 10^4 connections * 1fJ / 10^-4 efficiency of the source = 10^3 Joules
10^6 clockspeed * 10^-3 utilization (not all neurons firing at once) = 1Mwatt

## Slide 18: Energy estimates
10^10 neurons
10^10 * 10^4 connections
10^10 * 10^4 * 10^5 photons
10^19 photons * 10^4 inefficiency
10^23 photons = 10^23 eV = 10^4 J
1fJ = 1e-15J = 10 photons

## Slide 19
Fluxonic processing of photonic synapse events
Spiking neural networks
jeffrey.shainline@nist.gov

## Slide 20
Fluxonic processing of photonic synapse events
Light for communication

## Slide 21
Fluxonic processing of photonic synapse events
Superconducting electronics for single-photon detection

## Slide 22
Fluxonic processing of photonic synapse events
Superconducting electronics for neural computation

## Slide 23
Fluxonic processing of photonic synapse events
Neuromorphic supercomputing

## Slide 24
Device requirements for massive connectivity
Dense local fanout
Long-range connectivity
Principal conjecture:
Use light for communication
Photons don’t have charge or mass
We seek very large systems
Energy efficiency is paramount
Use single-photons for communication

## Slide 25
Neurons that signal with single photons

## Slide 26
Neurons that signal with single photons
How do they work?

## Slide 27
Superconducting loop

## Slide 28
Photons add current

## Slide 29
Current gets integrated

## Slide 30
Current threshold

## Slide 31
Current threshold

## Slide 32
Photons produced

## Slide 33
Synapse transduces

## Slide 34
Photons update weight

## Slide 35
Inhibitory synapses

## Slide 36
Many synapses

## Slide 37
Transmitter circuits

## Slide 38
Colors for different operations

## Slide 41
Loop neuron
Shainline et al., arXiv:1805.01929 (2018).
Shaineline, arXiv:1904.02807 (2019)

## Slide 42
Photon-to-fluxon transducer
these are fluxons

## Slide 43
The synapse

## Slide 44
Long-range = photons
Short-range = electronics / SFQ
https://arxiv.org/abs/1907.00263
A Power Efficient Artificial Neuron Using Superconducting Nanowires
Emily Toomey, Ken Segall, Karl Berggren
Pulsed neural networks consisting of single-flux-quantum spiking neurons
T. Hirose, T. Asai, and Y. Amemiya
Physica C, 463:1072, 2007.

## Slide 45: SOEN technical approach superconducting optoelectronic networks
Single photons for minimum spike energy
  (superconducting single-photon detectors )
2. Cold optoelectronics for monolithic integration
  (all-silicon light-emitting diodes)
3. Cold electronics (SFQ) for nonlinear processing
  (Josephson junctions, cryotron switches)
4. Light for interconnects
  (silicon photonics)
1.
2.
3.
4.
J. M. Shainline, S. M. Buckley, R. P. Mirin, and S. W. Nam, “Superconducting optoelectronic circuits for neuromorphic computing,” Phys. Rev. Applied, Mar 2017.
Notes: Accepting to work at cryogenic temperatures means other devices become available

## Slide 46: cryogenic silicon photonics platform: recent results

## Slide 47
Superconducting Nanowire Detector
single photon
160 nm
5 nm
Waveguide
Nanowire on waveguide

## Slide 48: All-silicon light emitting diodes
Si defect centers have optical transitions
Low temp. inhibits non-radiative pathways
Electrical pumping with PN junction
W-centers: 1220nm emission
S. M. Buckley et al. “All-silicon light-emitting diodes waveguide-integrated...” APL, 2017.
Notes: Describe the fabrication briefly

## Slide 49: Co-integration: Silicon LEDs + SNSPDs
S. M. Buckley et al. “All-silicon light-emitting diodes waveguide-integrated...” APL, 2017.
Notes: Say that: since this article, we have enhanced photoluminescence by a factor of 300. Promising results and a paper is in preparation.

## Slide 50: All-silicon light emitting diodes
LED turn-on voltage is ~ 1 V
SNSPD can output ~ 1 mV
S. M. Buckley et al. “All-silicon light-emitting diodes waveguide-integrated...” APL, 2017.
Notes: Describe the fabrication briefly

## Slide 51: Nano-cryotron thermal switch
millivolt input -> Volt output
No Josephson Junctions needed
Reset about 10ns
A. McCaughan et al. “A compact, ultrahigh impedance superconducting thermal switch for interfacing superconductors with semiconductors and optoelectronics,” arXiv:1903.10461, 2019.

## Slide 52: Superconductor-to-semiconductor interface
4.6 us
Time (us)
A. McCaughan et al. “A compact, ultrahigh impedance superconducting thermal switch for interfacing superconductors with semiconductors and optoelectronics,” arXiv:1903.10461, 2019.
Notes: What points to make about this

## Slide 53: First steps toward photonic networks
Three planes of amorphous silicon waveguides
Chiles et al., APL Photonics 2, 116101 (2017)

## Slide 54
Inter-planar couplers
0.05 dB loss
36 mm length
36 mm
Chiles et al, APL Photonics 2 116101 (2017).

## Slide 55
10 x 100 routing couplers
Chiles et al, APL Photonics 3 106101 (2018).

## Slide 56
10 x 100 routing couplers

## Slide 57
10 x 100 routing couplers

## Slide 58: Full Superconducting Optoelectronic Neuron
Optical
Optical
Fluxonic
SNSPDs
Silicon LED
Josephson
Junction circuits
Electronic
Electronic
Superconducting
Switch
J. M. Shainline, “Fluxonic processing of photonic synapse events,” arXiv:1904.02807, 2019.
Notes: photons are expensive
one circuit multiple purposes (enumerate some)
summing and intermediate processing
Come back to characteristic length. We should pack a bunch of complexity in a small space and make it electronic

## Slide 59: Eventual transfer to 300 mm foundry
Notes: And for better scale

## Slide 60
Fabricated at SUNY Poly by Pops Papa Rao and team
Measured at NIST by our team
Light sources on 300-mm wafers
Photoluminescence of W centers in Si at 4 K

## Slide 61
Wafer-scale modules

## Slide 62: Free-space interconnects for 3D

## Slide 63
Free-space inter-wafer interconnects

## Slide 64
Multi-wafer modules

## Slide 65
Brain-scale systems?
> 100 Billion neurons

## Slide 66
What can we do in five years?
Artificial visual cortex

## Slide 67
Dense local fan-out with photonics
Long-range communication at light speed
Computing and memory with superconducting electronics
Superconducting
optoelectronic
networks
Would this reach the limits of cognition?

## Slide 69: Summary
Low Temperature Devices have the potential to be important in super-neuromorphic computing
Can we get to a size scale for “Cognitive” Systems?
Light for communication
Superconductors for computation
Complex neuro circuits

## Slide 70: NIST team
Rich Mirin
Jeff Shainline
Sonia Buckley
Adam McCaughan
Alex Tait
Jeff Chiles
Saeed Khan
Krister Shalm
Marty Stevens
Adriana Lita
Varun Verma
Nima Nader
Mike Mazurek
Dileep Reddy
Eric Stanton
Galen Moody
Kevin Silverman
Thomas Gerrits
Boulder Labs
saewoo.nam@nist.gov
MIT, JPL, Suny-Poly

## Slide 71
Cryogenic sensors

## Slide 72
Collider readout

## Slide 73
Genetic analysis

## Slide 74
Neuroscience

## Slide 75
Traffic networks

## Slide 76
Data centers

## Slide 77
Quantum interface

## Slide 78: Quantum-neural hybrid systems
Quantum systems:
Inherently probabilistic
Quantum computing statistical
Entanglement fragile
Difficult to scale
Neural systems:
Sample probability distributions
Perform Bayesian inference
Spiking information robust
Highly scalable
What can a neural system know about a quantum system?

## Slide 79: Structure of a Biological Neuron
http://spie.org/news/5681-dendritic-plateau-potentials-modulate-neuronal-function?SSO=1
From:Wikipedia

## Slide 80
S
F(x)
w1
w2
w3
x1
x2
x3
b
Summing
Node
Synaptic
Weights
inputs
Activation
Function

## Slide 81: Supervised Learning
https://abeyon.com/how-do-machines-learn/
Use “labeled” data to determine weights and biases in a neural network
Make “inferences” on new inputs

## Slide 83
https://towardsdatascience.com/spiking-neural-networks-the-next-generation-of-machine-learning-84e167f4eb2b

## Slide 84
The synapse

## Slide 87
McCaughan et al., “A Superconducting-Nanowire Three-Terminal Electrothermal Device”, Nano Lett. (2014)

## Slide 89
McCaughan et al., in preparation

## Slide 91
Requirements for light sources
Incoherent pulses
~10,000 photons per pulse (fJ)
Efficiency of 10-3
20 MHz
4.2 K

## Slide 92: The basic SOEN neuron
Cryotron
Switch
Silicon LED
Optical
Optical
Electronic
SNSPD
input
input
SNSPD
output
J. M. Shainline, S. M. Buckley, R. P. Mirin, and S. W. Nam, “Superconducting optoelectronic circuits for neuromorphic computing,” Phys. Rev. Applied, Mar 2017.
1 photon
1 mV
1 V
10,000 photons
Notes: Point about O/E/O
Optical nonlinerity would need a ton of power
Summing in the electronic domain
We have shown these things separately. We are working now on co-integration

## Slide 93: Co-integration: waveguides + SNSPDs
1 um
J. Shainline et al. ” Room-temperature-deposited dielectrics and superconductors for...” Op. Ex., 2017.
Notes: No dark counts
High yield
Photonic routing

## Slide 94: Recap: The basic SOEN neuron
Cryotron
Switch
Silicon LED
Optical
Optical
Electronic
SNSPD
input
input
SNSPD
output
J. M. Shainline, S. M. Buckley, R. P. Mirin, and S. W. Nam, “Superconducting optoelectronic circuits for neuromorphic computing,” Phys. Rev. Applied, Mar 2017.
1 photon
1 mV
1 V
10,000 photons
Notes: Point about O/E/O
Optical nonlinerity would need a ton of power
Summing in the electronic domain
We have shown these things separately. We are working now on co-integration

## Slide 95: Fluxonic processing
Flux induced by excitatory SNSPDs
Flux induced by inhibitory SNSPD
Flux induced in the next junction
Weighted sum of incoming fluxes
Inductive coupling
to LED
J. M. Shainline, “Fluxonic processing of photonic synapse events,” arXiv:1904.02807, 2019.
Notes: Fan-in
Cascadability
Programmability

## Slide 96: Fluxonic processing
Flux induced by excitatory SNSPDs
Flux induced by inhibitory SNSPD
Flux induced in the next junction
Weighted sum of incoming fluxes
Inductive coupling
J. M. Shainline, “Fluxonic processing of photonic synapse events,” arXiv:1904.02807, 2019.
Notes: Fan-in
Cascadability
Programmability

## Slide 97
Camera Measurements
Optical Fiber
Grating
couplers
View through camera
Single fiber input
Measure many ports

## Slide 98: Sources + detectors + readout  generic testbed
SNSPDs
Superconducting
switches
Silicon LED
Your Circuit Here
Public multi-project wafer (MPW) offering is planned
We are looking for collaborators on MPW pre-pilot runs
  Need experimental capabilities and application ideas (esp. in quantum)
  More info pages.nist.gov/SOEN-PDK
  Contact jeffrey.shainline@nist.gov, alexander.tait@nist.gov
S. Papa Rao. “Progress Towards Enabling Quantum Engineering.” PfQ Workshop, RIT, Jan. 2019.
http://ridl.cfd.rit.edu/products/talks/PfQ/Friday/PfQ%20Pops.pdf
Notes: Part of NISTs mission is to promote innovation and industry,
not just through our research but by enabling others to do their research

## Slide 99
SUNY Poly for process at 300 mm scale
Path to full integration at large scales

## Slide 100: Summary
Foundry silicon photonics enables new concepts in information processing now
The SOEN proposal
  What are the physical limits to large-scale neuromorphic systems
Recent co-integration results
  SNSPDs
  All-silicon LEDs
  Superconducting switches
  Multi-planar waveguides
  Fluxonic circuitry
Cryogenic silicon photonics MPW

## Slide 101
Can’t we do all this at room temperature?
Yes, but
Source efficiency improves 100x at 4 K
Detector efficiency improves 100x at 4 K
Superconducting circuits excel at neuro
Communicate to 300 K with 1 eV photons
Quantum-neural hybrid computing

## Slide 102
Why neurons?
Energy efficient
Tunable frequency response
Resilient to noise
Information in rate and correlations

## Slide 103
Synaptic transducer

## Slide 105
Lowest light level
(hν = 1.3 x 10-19 J)

## Slide 106
Lowest light level
Zero static power

## Slide 107
Synaptic transducer

## Slide 108
Synaptic transducer

## Slide 109
Synaptic transducer

## Slide 110
Synaptic bias current
Synaptic transducer

## Slide 111
Dendritic processing
Coincidence detection

## Slide 112
Dendritic processing
Sequence detection

## Slide 113
Dendritic processing
Nonlinear processing

## Slide 114
Transmitters

## Slide 115
Waveguide-coupled electroluminescence from silicon
W-center emission
To taper

## Slide 116
Emitters integrated with single-photon detectors
Buckley et al, APL 111 141101 (2017).

## Slide 117
Requirements for light sources
Incoherent pulses
10,000 photons per pulse (fJ)
Efficiency of 10-3
20 MHz
4.2 K
Should be pretty easy

## Slide 118
How do we implement photonic networks?

## Slide 119: First steps toward photonic networks
Three planes of amorphous silicon waveguides
Chiles et al., APL Photonics 2, 116101 (2017)

## Slide 120
Inter-planar couplers
0.05 dB loss
36 mm length
36 mm
Chiles et al, APL Photonics 2 116101 (2017).

## Slide 121
10 x 100 routing couplers
Chiles et al, APL Photonics 3 106101 (2018).

## Slide 122
Core device
Tap and transition

## Slide 123
10 x 100 routing couplers

## Slide 124
10 x 100 routing couplers

## Slide 125
10 x 100 routing couplers

## Slide 126
10 x 100 routing couplers

## Slide 127
10 x 100 routing couplers

## Slide 128
Camera Measurements
Optical Fiber
Grating
couplers
View through camera
Single fiber input
Measure many ports

## Slide 129
Camera Measurements
Optical Fiber
Grating
couplers
View through camera
Analogous to MRI
Volume imaging of 3D assemblies

## Slide 130
Further scaling to 3D

## Slide 131
Waveguide routing architecture

## Slide 132
Waveguide routing architecture

## Slide 133
Calculate the area:
1 cm x 1 cm die: 8100 neurons + 300,000 synapses
300 mm wafer: 1 million neurons + 200 million synapses

## Slide 134
Calculate the area:
1 cm x 1 cm die: 8100 neurons + 300,000 synapses
300 mm wafer: 1 million neurons + 200 million synapses

## Slide 135
Differentiated local processing
Information integration across:
  Space (network structure)
  Time (dynamics)
  Experience (plasticity)
Cognitive Systems:

## Slide 136
Differentiated local processing
Information integration across:
  Space (network structure)
  Time (dynamics)
  Experience (plasticity)
Cognitive Systems:

## Slide 137
Time and space intertwined
High-frequency oscillations synchronize local sectors

## Slide 138
Time and space intertwined
High-frequency oscillations synchronize local sectors
Mid-frequency oscillations synchronize regions

## Slide 139
Time and space intertwined
High-frequency oscillations synchronize local sectors
Mid-frequency oscillations synchronize regions
Low-frequency oscillations synchronize the system

## Slide 140
Time and space intertwined
Need neurons that can oscillate across many frequencies

## Slide 141
Time and space intertwined
Need neurons that can oscillate across many frequencies
Brain: up to 600 Hz

## Slide 142
Time and space intertwined
Need neurons that can oscillate across many frequencies
Brain: up to 600 Hz
Loop neurons: up to 20 MHz

## Slide 143
Time and space intertwined
What if you could think 30,000 times faster?

## Slide 144
Synaptic update

## Slide 145
Synaptic plasticity
Adaptive memory at each synapse

## Slide 146
Supervised learning

## Slide 147
Supervised learning
Analog synaptic weights

## Slide 148
Unsupervised learning
Two photons for spike-timing dependent plasticity
Complex circuit functionality
Weighting in the superconducting domain conserves photons

## Slide 149
Other plasticity mechanisms
Short-term plasticity

## Slide 150
Other plasticity mechanisms
Homeostatic
plasticity

## Slide 151
Other plasticity mechanisms
Metaplasticity

## Slide 152
Weaknesses:

## Slide 153
Process development
3”
NIST cleanroom for near-term results

## Slide 154
Process development
NIST cleanroom for near-term results
SUNY Poly for development of optoelectronic process at 300 mm scale

## Slide 155
NIST should share their process

## Slide 156
NIST should share their process
We agree.

## Slide 157
NIST should share their process
We agree. We’re working on it.

## Slide 158
NIST should share their process
Silicon light sources, single-photon detectors, passive dielectric waveguides

## Slide 159
NIST should share their process
Process design kit and multi-project wafers, hopefully 2019
let me know if you’re interested
jeffrey.shainline@nist.gov

## Slide 160
Weaknesses:
Requires process development
Cryogenic operation

## Slide 161
Weaknesses:
Requires process development
Cryogenic operation

## Slide 162
Weaknesses:
Requires process development
Cryogenic operation
(minor inconvenience)

## Slide 163
Can you find the fridge?

## Slide 164
Can you find the fridge?

## Slide 165
Ultimate scaling limits

## Slide 166
Number of neurons capable of synchronizing
Ultimate scaling limits

## Slide 167
The neuronal pool
Number of neurons capable of synchronizing

## Slide 168
1010 times the number of synapses as the brain
Operating 30,000 times faster
Very large cognitive systems

## Slide 169
Superconducting optoelectronic networks
Light for communication
Superconductors for computation
Complex neuro circuits
arXiv:1805.01929
arXiv:1805.01947
jeffrey.shainline@nist.gov

## Slide 170
Quantum-neural hybrid computing

## Slide 171
Can’t we do all this at room temperature?
Yes, but
Source efficiency improves 100x at 4 K
Detector efficiency improves 100x at 4 K
Superconducting circuits excel at neuro
Communicate to 300 K with 1 eV photons
Quantum-neural hybrid computing

## Slide 172
Why neurons?
Energy efficient
Tunable frequency response
Resilient to noise
Information in rate and correlations